Model #:			2070716-1

Description:		Finger Tip Abrasion Tester

Date:                                MARCH 2009

Sequence of Operations

- Plug test machine in to 115 volt 60Hz. power source.

- Turn the main power switch “ON”.

- The speed of the machine may need to be adjusted. To check, press the green “START” button and time the number of cycles in one minute and then press the “STOP” button. If the cycle count is OK, continue, if not see the speed adjustment page in this manual.

Test Procedure Set Up

- Measure test specimen thickness and record.

- Rotate Finger Cam Arm (#3) so that finger is in the up position.

- Make sure the specimen holding clamps ($13) are open.

- Position test specimen under holding clamps ($13) and clamp down. Note: specimen should be in line with the top of machine.

- Loosen (3) star knobs ($3) and lift the Finger Tip Drive Assembly.

- Place appropriate combination of shims ($5, 6 & 7) equal to the specimen thickness between the Height Set Block (#4) and the Finger Tip Drive Assembly.

- Lower the drive assembly onto shims and tighten knobs to set machine at proper operating position.

- Open abratent holding clamp ($4).

- Position Abradent swatch under clamp, on the test specimen and in line with the abradent holding mechanism.

- Close the abradent holding clamp.

- Attach the tensioning clip, weight and string to the end of the abradent swatch and hang over guide arm (#7). Note: configure abradent swatch so that abradent material is between the tensioning clip and the test specimen to eliminate unnecessary marking of the specimen. This may require making the abradent swatch longer or attaching a small piece of material to the clip.

- Remove “O” ring from end of finger.

- Wrap the end of the finger with the appropriate felt material.

- Replace the “O” ring making sure no creases are in the tip of the finger.

- Test specimen, abradent and finger are now ready for test.

Running The Test

- Set the counter to the desired number of cycles. (See Counter Operating Instructions included with this manual)

- Press the green “START” button to begin the Finger Tip Abrasion Test

- Watch the procedure for at least one minute to make sure everything is running correctly. The abradent holding mechanism takes one minute to make one complete cycle.

- When the number of cycles is complete, the tester will automatically stop.

- The red button on the counter must be pushed to reset the counter before a new test can be run.

- Pushing the red “STOP” button will stop the test at anytime (Count does not reset). Pressing the green “START” button resumes the test.

- When test is done, remove tensioning clip, abradent material and test specimen.

- Evaluate test specimen.

- When testing is done, turn the power switch to “OFF” and unplug the test machine.