OPERATING INSTRUCTIONS

### FLEX TESTER

#205305

# OPERATING INSTRUCTIONS

- Cut 1 to 14 samples as required for testing. Sample size is 3 ½” x 4 ½”.

- Manually index machine until one of the parallel shafts is at maximum stroke.

- Loosen the hose clamps in the number of locations that there are specimens to be tested.

- Place specimens around the locations that are in the widest position.

- Tighten clamps to secure.

- Manually index machine 180 degrees until the alternate shaft locations are at the maximum stroke.

- Place remaining specimens around these locations.

- Tighten clamps to secure.

- Turn the power to the machine “ON”.

- Preset the desired number of cycles on the Durant cycle counter (see instructions).

- Press the “RST” button on the counter to start (Note: the machine may be turned off at any time by turning the power “OFF”.  When power is turned “ON”  the test and count will continue).

- The tester will automatically stop at the preset number on the cycle counter.

- Remove specimens and examine.

- Pressing the reset key on the cycle counter will start another test.  Display will clear then run up to previously set number of cycles.

# CYCLE COUNTER PRESET INSTRUCTIONS

- Press the “SEL” key so “P1” is displayed.

- Use the key under each digit to change that value. Display will show new preset value.

- Press the “SEL” key again to exit.

- Press “RST” to start test.

#### PREVENTITIVE MAINTNANCE

This machine requires lubrication every 400 hours of operation or once every three months, whichever comes first.

- Remove cover.

- Lubricate both pillow block bearings using a good quality, medium viscosity, all-purpose grease.

- Lubricate two open cam bearings with fingers using the same grease.

- Reinstall guard.

- Linear bearings do not require periodic lubrication.