SCHAP Model # 2100127

Scott-Type Crease Flex Tester

Operator Instructions

- Turn Power button to the “ON” position.

- Press Jog button to align the crank of the adjustable

stroke slide, so it is visible & centered in the clear lexan door.

- Open the clear lexan door to access the adjustable stroke slide. Note: machine will not run when door is open

- Turn the crank handle clockwise or counter-clockwise to the desired length of

test stroke specified in the test specifications. Close door.

- Set the desired Chuck width opening as specified in the test procedure using the Crank handle on the left side of the tester.

- Open cover to access clamping mechanism. Note: Machine will not run when cover is open.

- Open the jaws of the specimen grips to approximately 15mm.

- Load the prepared test specimens into the grips per instructions in test specifications.

- Tighten specimens securely in the grips using the (2) knurled clamping knobs.

- Close the Chuck with the Crank handle on the left side ensuring that the samples bend away from each other.

- Apply additional abrasion load by continuing to rotate the crank handle on the left side. The spring loaded mechanism uses a rate of approximately 1 N per mm, but it is not exact. The customer needs to calibrate the actual abrasion preload applied that corresponds to the scale& pointer as provided.

- Program the Eaton Counter/Timer to the number of test cycles, per test Spec.

(See the E5148C1421 counter setting instructions in this manual)

- Close cover to secure machine for test.

- Push the green Start button to begin the test cycle, the test will stop automatically

when the programmed number of test cycles is reached.

- Push the red Stop button to stop the test at any time.  Stopping the test will not

re-set the counter, the test may be resumed by pushing the green Start button.

The test can only be re-set by using the counter re-set button.

4/01/10  JRB