SET-UP AND SEQUENCE OF OPERATION

## SINGLE STATION PILLING TESTER

(205304)

# SET-UP

Note: The set-up procedure is required when the preset number on counter is to be changed.

- Press the button below the digit you want change.

- Keep pressing the button until the desired number is shown.

- Continue process until desired preset value is shown.

# SEQUENCE OF OPERATION FORD BN 108-03

- Position the test specimen in spring loaded specimen holder using rubber coated bars.

- Position the brush board on the test machine.

- Place the specimen holder over the brush board.

- Set the desired number of cycles on the counter (note: one cycle is approximately one second long).

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- You must press the RST button on the counter before you can start the cycle again.

- Remove the specimen holder and replace the brush board with the sponge board.

- Place the specimen holder over the sponge board.

- Set the desired number of cycles on the counter.

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- You must press the RST button on the counter before you can start the cycle again.

- Remove the specimen holder and replace the sponge board with the velcro board.

- Place the specimen holder over the velcro board.

- Set the desired number of cycles to run on the counter.

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- Evaluate the test specimen.

# SEQUENCE OF OPERATION FORD BN 108-14

- Position the test specimen in specimen holder on the weight assembly.

- Position the pilling board (wood block) on the test machine.

- Position the abradant on the pilling board (wood block).

- Place the specimen holder/weight assembly on the pilling board with appropriate amount of weight.

- Set the desired number of cycles on the counter (note: one cycle is approximately one second long).

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- Evaluate the test specimen.

# SEQUENCE OF OPERATION ASTM D 3511-02

- Position the test specimen in the specimen holder disk and secure with “O” ring.

- Position the brush board on the test machine.

- Place the specimen holder over the brush board.

- Set the desired number of cycles on the counter (note: one cycle is approximately one second long).

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- You must press the RST button on the counter before you can start the cycle again.

- Remove the specimen holder and replace the brush board with the fixed sample holder disk.

- Position a second test specimen on fixed sample holder disk and secure with “O” ring.

- Place the specimen holder over the fixed sample holder.

- Set the desired number of cycles on the counter.

- Press the cycle start button.

- The tester will stop after the preset number is reached.

- Evaluate the test specimen.